## Problem to: Subchapter 3.2.3 “Ionic Polarization”

Filename; Title: p3_2_3-1; “Ionic polarization”

| ## Info |  |
| --- | --- |
| Used: | Exam spring 05 |
| Points. |  |

| a) | b) |
| --- | --- |
| Fig. 1: a) NaCl crystal structure. b) Optical reflection spectra of NaCl in the far IR regime. |  |

a) 	Explain qualitatively how ionic polarization works!  What are the opposing forces? What is the connection to phonons?

b) 	How do lattice atoms move when an acustic, resp. optical phonon is excited? Which type of phonon can thus be only responsible for ionic polarization?

#### Addition for 3.7”Dielectrics and Optics”

Fig. 1(b) shows the measured optical reflectance of NaCl in the far infrared (FIR).

g) 	How are transmission T, absorption A, and reflection R connected?

h) 	Is a peak in the reflection an automatic sign of a resonance in the dielectric function ?

Assume for the rest that the reflection peak in Fig. 1b is indeed caused by a resonance phenomena!

i) 	Determine the wavelength  and frequency f of the major reflection peak at 25 meV! Is this a typical phonon energy? Compare these values with your theoretically calculated ones from e)!