## Slide 1: Quantum Dot Infrared Photodetectors
Hackeem Owusu Sushobhan Joshi
Notes: <number>

## Slide 2: Outline
Introduction
Quantum Dots (QDs)
Quantum Dot Infrared Photodetectors (QDIPs)
Tailoring of QD Electronic Energy Levels and Wave Functions
QDIP Device Characteristics
  Dark Current
  Responsivity
  Noise
  Photoconductive gain
  Detectivity
Applications

## Slide 3: Introduction Shortcomings of Traditional Semiconductors
Traditional (bulk) semiconductors (S/Cs) lack versatility
Their optoelectronic qualities are costly to adjust
Their bandgap cannot be easily changed
Their emission frequencies cannot be easily manipulated by engineering

## Slide 4: Introduction Shortcomings of Traditional Semiconductors
Moore’s law: “that the density of transistors on a silicon chip will double every three years”
Demands the ability to continue miniaturizing the transistors in chips
Problems surface in forms of:
  the thickness of the oxide layer (already only a few nanometers)
  the size of the gate of the transistor (if in nanoscale, there could be leakage across it due to tunneling of electrons)
  limits on the lithography processes

## Slide 5: Introduction Nanostructure Based Semiconductors (S/C)
Semiconductors that use the quantum mechanical effects
Allow the shrinking of devices to sizes of only a few nanometers
Unparalleled in versatility and flexible in form
Allows us to make semiconductors with tunable bandgaps

## Slide 6: Introduction Quantum Confinements
Electrons in S/C nanostructures have a range of energies although the concepts of energy levels, bandgap still apply.
Exciton Bohr Radius (avg. gap between electron and hole), is different for each material.
In nanostructure (eg. QDs), the dimension of the crystal is smaller enough to disallow Exciton Bohr radius to extend to full fledge.
The electron energy levels can no longer be treated as continuous but as discrete, meaning that there is a small and finite separation between energy levels.
This situation of discrete energy levels is called quantum confinement, where, the semiconductor material ceases to resemble bulk.

## Slide 7: Introduction Quantum Confinements
  One Dimensional – Quantum Well; which confines the motion of electrons or holes or excitons in one dimension and allow free propagation in two dimensions
  Two Dimensional – Quantum Wire; which confines the motion of electrons or holes or excitons in two spatial dimensions and allow free propagation in the third
  Three Dimensional – Quantum Dot; in all three spatial directions

## Slide 8: Introduction Quantum Confinements’ Causes
The confinement can be due to electrostatic potentials (generated by external electrodes, doping, strain, impurities)
The presence of an interface between different semiconductor materials (e.g. in quantum wells; a very thin layer of a semiconductor sandwiched between two layers of another semiconductor with wider energy gaps)
The presence of the semiconductor surface, or a combination of these

## Slide 9: Introduction Optoelectronic Devices Based on S/C Nanostructures
Quantum Well Lasers (1970s)
Quantum Dot Infrared Detectors (QDIPs)
Quantum Dot Lasers
Tunnel Injection QD Lasers
(Possibly in future)
Quantum Dot Solar Cells
Fluorescence Spectroscopy (detecting tumors)
QD Light Emitting Diodes
QD Displays
QD Transistor and hence QD Computer

## Slide 10: Quantum Dots (QDs)
S/C nanostructures that confines the motion of conduction band electrons, valence band holes, or excitons in all three spatial directions.
As electron energy levels are discrete in QDs, the addition or subtraction of a few atoms to the QD has the effect of altering the boundaries of the bandgap.
Therefore the size of the bandgap is controlled simply by adjusting the size of the dot
Changing the geometry of the surface of the QD also changes the bandgap energy.

## Slide 11: Quantum Dots Fabrication
If one S/C is grown on another under strain (GaAs/AlGaAs), the strain results in the spontaneous formation of small islands
These islands are about the right size to act as QDs near room temperature.

## Slide 12: Quantum Dots Growth Technique
The most commonly used techniques for the growth of uniform arrays of 3 dimensional QDs
are:
  Molecular Beam Epitaxy (MBE)
  Metalorganic Chemical Vapor Deposition (MOCVD)
Both lattice-matched and lattice-mismatched (heteroepitaxial) systems can be used for the formation of nanostructures
In a lattice-mismatch as a GaAs/InAs heterostructure, as the critical thickness is exceeded, formation of randomly distributed islandstakes place.

## Slide 13: Quantum Dots Molecular Beam Epitaxy
The epitaxial growth takes place through reactions between the atomic / molecular beams of the source materials and the substrate surface.
The system is heated to a certain temperature in an ultrahigh vacuum environment.
Gases can also be used as potential precursor sources, generally for group V elements in the synthesis of III-V compounds

## Slide 14: Quantum Dots Metalorganic Chemical Vapor Deposition
Ability to produce high-quality epitaxial layers with thicknesses as thin as a few atomic layers
Growth process is based on the pyrolysis of alkyls or metalorganics (of group III elements typically) in an atmosphere of hydrides (of group V elements typically)
Controlled amounts alkyls and hydride gases are introduced into a reaction chamber in which a S/C substrate is placed on a heated susceptor
S/C crystal growth takes place in this hot region due catalytic effect on the decomposition of the gaseous products

## Slide 15: Quantum Dots Schematic Diagram (MOCVD)

## Slide 16: Quantum Dots Growth Modes
Frank-van der Merwe
Volmer-Weber
Stranski-Krastanov

## Slide 17: Quantum Dots Materials
Chief materials of which QDs are composed of belong to periodic groups of II-VI, III-V, or IV-VI materials.

## Slide 18: Quantum Dots Infrared Photodetector self-assembled QDs (SAQDs)
As infrared (IR) photodetectors in the near-IR to long-IR wavelength (1- to 20-μm) regime.
Generally (InGaAl)/As family

## Slide 19: Quantum Dots Infrared Photodetector Shape of the Qds
Schematic of (a) a buried pyramidal island and (b) the conduction and valence band edge lineup that defines the confinement potential along the line passing through the island base.
The tapering toward the apex symbolizes lower compressive strain toward the apex.
The 3D quantum confined states, arising from the full 3D confinement potential, are indicated along with the interband and intraband transitions to be tailored for detectors.

## Slide 20: Quantum Dots Infrared Photodetector Energy Band Characteristics
In such spatially varying potential, the electrons and holes in certain regions acquire spatially confined wave functions along with discrete energies.
Limitations on the matching of the dominant optical phonon energies with the range of energy relaxation to the ground state following excitation of an electron to a higher state introduces a so called “phonon bottleneck”
This enhances the excited carrier lifetime.
Helpful for collection of the carriers as photocurrent and for achieving high photoconductive gain.

## Slide 21: Quantum Dots Infrared Photodetector Device Structure
Depending on transport direction,two types of structures can be used for QDIPs:
Lateral Transport Structure
AlGaAs barriers are utilized to modulation-dope the quantum dots and to provide a high-mobility channel
Vertical Transport Structure

## Slide 22: Tailoring of QD Electronic Energy Levels and Wave Functions

## Slide 23: Tailoring of QD Electronic Energy Levels and Wave Functions
Typically, NIR PC peaks are much less resolved at LHe temperatures due to decreased probability of carrier extraction and thus suppressed photocurrent.
Due to the integrative nature of photocurrent detection, as opposed to the size subensemble selection in PLE, one resolves only the strongest transitions in the presence of inhomogeneous broadening
the intraband transitions give much richer information on the electronic structure

## Slide 24: Tailoring of QD Electronic Energy Levels and Wave Functions

## Slide 25: Tailoring of QD Electronic Energy Levels and Wave Functions
According to the calculated energy levels in pyramidal InAs/GaAs QDs, one would expect a much richer PC level structure than the two detected peaks
Also some allowed transitions might not be observed due to small oscillator strengths or due to the shallow depth of the higher energy levels involved
The inhomogeneity caused by the QD size fluctuation causes broadening of transition energies and thus compromises resolution

## Slide 26: Tailoring of QD Electronic Energy Levels and Wave Functions

## Slide 27: Tailoring of QD Electronic Energy Levels and Wave Functions

## Slide 28: Tailoring of QD Electronic Energy Levels and Wave Functions

## Slide 29: AlGaAs Capped Large InAs MQD QDIP Structures
The real trade-off is between the number of QD layers and the total strain buildup that increases structural defect density
Operationally, the considerations are between the size of the islands, the lattice mismatch with the capping layer, and the thickness of the capping layer
It is routine now to exploit the buried island induced stress fields on the cap layer surface to achieve considerable vertical self-organization (VSO) of the SAQDs,

## Slide 30: AlGaAs Capped Large InAs MQD QDIP Structures

## Slide 31: Probe for QDIPs

## Slide 32: Probe for QDIPs

## Slide 33: Probe for QDIPs

## Slide 34: InxGa1-xAs Capped Small and Large InAs MQD-Based QDIP Structures
Large InAs/GaAs/AlGaAs QDIP structures allow considerable reduction in the dark current due to the AlGaAs blocking layers, the photoresponse is restricted to the 5- to 7-µm regime
Manipulating the QD quantum confinement potential via change in the barrier GaAs layer to alloy InGaAs

## Slide 35: Tailoring the Electronic Structure of the QDs
The chemical effect of In lowering the band edges and thus the band discontinuities that define the confinement potential,
The accompanying reduction in the lattice mismatch between the InAs island material and the InGaAs capping layer lowering the strain and thus the band edge discontinuities.

## Slide 36: QDIP Device Characteristics
The detectivity, D*, of these devices was three to four orders of magnitude lower than QWIPs with similar structures
QD layers have less than unity fill factors The net result is lower responsivity of the QDIPs
Another limiting factor for the QDIPs is that they have exhibited higher dark current that is comparable to or even higher than that of QWIPs

## Slide 37: Applications of QDIP
The development of quantum dot infrared photodetectors technology that may provide new imaging techniques with applications:
In medical and biological imaging,
Environmental and chemical monitoring,
Night vision and infrared imaging from space.

## Slide 38: Imaging Systems
Conventional infrared photon detector technology for imaging applications typically requires that the detector be cooled to very low temperatures
Quantum Devices are one step closer to achieving the goal of developing high-performance imaging techniques that can operate at higher temperatures.

## Slide 39: References:
“Semiconductor Nanostructures for Optoelectronic Applications”, Todd Steiner, 2004 ARTECH HOUSE, INC.
“NANOSTRUCTURES & NANOMATERIALS, Synthesis, properties & Applications”, Guozhong Cao, 2004 by Imperial College Press
“Quantum dot infrared photodetector”, H.C. LIU, OPTO-ELECTRONICS REVIEW 11(1), 1–5 (2003)
“Theoretical analysis of quantum dot infrared photodetectors”, Mashade et. al, INSTITUTE OF PHYSICS PUBLISHING SEMICONDUCTOR SCIENCE AND TECHNOLOGY
Semicond. Sci. Technol. 18 (2003) 891–900
http://www.sciencedaily.com/releases/2007/05/070517120153.htm
http://www.evidenttech.com/quantum-dots-explained.html
http://www.cmmp.ucl.ac.uk/~mjg/index.html
http://en.wikipedia.org/wiki/Quantum_dot

## Slide 40
Thank You !