## Slide 1: Polymer Semiconductors
By:
Tania Claudio &
Sebastian Dollinger

## Slide 2: Outline
History
Principles
Devices
References

## Slide 3: History
1953 - Staudinger - Nobel Prize in Chemistry - “for his discoveries in the field of macromolecular chemistry”;
1963 - Ziegler and Natta - Nobel Prize in Chemistry - “for their discoveries in the field of the chemistry and technology of high polymers”;
1974 - Flory - Nobel Prize in Chemistry - “for his fundamental achievements, both theoretical and experimental, in the physical chemistry of macromolecules”.
Saturated Polymers
Conjugated Polymers
1991 - Professor Bengt Rånby designated electrically conducting polymers as the “fourth generation of polymeric materials”
Notes: 1920s - Hermann Staudinger developed the concept of macromolecules;
1935 - Wallace Carothers (DuPont) invented nylon;
1950s - Karl Ziegler and Giulio Natta - polymerization catalysts;
1953 - Paul Flory - published his book, Principles of Polymer Chemistry

## Slide 4: Saturated x Conjugated
Saturated polymers - all of the four valence electrons of carbon are used up in covalent bonds
Conjugated polymers - the chemical bonding leads to one unpaired electron (the π-electron) per carbon atom
π-bonding - electron delocalization along the backbone of the polymer - “highway” for charge mobility
Result of π-bonding
Polymers can exhibit semiconducting or even metallic properties
The electronic structure determined by the chain symmetry (the number and kind of atoms within the repeat unit)

## Slide 5: Band Theory
Structure is dimerized due to Peierls instability
π-band divided into π- and π*-bands (each hold two electrons - spin up and spin down)
π-band is filled and the π*-band is empty
Energy difference is the π–π* energy gap, Eg
Notes: Energy difference between the highest occupied state in the π-band and the lowest unoccupied state in the π*-band is the π–π* energy gap, Eg
Since there are no partially filled bands conjugated polymers are typically semiconductors. Because Eg depends upon the molecular structure of the repeat unit, synthetic chemists are provided with the opportunity and the challenge to control the energy gap by design at the molecular level.

## Slide 6: Conduction Mechanisms
Solitons (Free radical defect):
break in pattern of bond alternation
relatively stable: charge of unpaired electron spreads over several monomer units
located in non-bonding state in middle of energy gap
Polarons
Localized electron or hole polarizes local environment
  relaxation of local structure
Polaron: defect consisting of deformed chain section and charge carrier
Bipolaron: pair of polarons
Chemical equivalents: radical ion and radical di-ion
Polaron movement: by thermally activated hopping

## Slide 7: Doping

## Slide 8: Doping
Fermi level moved by a redox reaction or an acid–base reaction
Reducing: analogous to donation of e- to conduction band (n-type)
  Redox reaction - formation of polymer salt by:
  a) immersing polymer in solution of the regent,
  b) electrochemical methods.
Oxidizing: analogous to removal of e- from valence band (p-type)
1. step: formation of cation radical
2. step: formation of dication

## Slide 9: Doping
Electrical conductivity of trans-(CH)x as a function of (AsF5) dopant concentration. The trans and cis polymer structures are also shown.

## Slide 10: Structures and conductivity of some doped conjugated polymers

## Slide 11: Conductivity in Polymers
Conductive polymers:
Conjugated
Doped
Electron movement
Along chains
Between chains

## Slide 12
Devices
History
Principles
Devices
References

## Slide 13
In Principle the whole field of electronic devices can be realized with polymers1.
For example:
organic field effect transistors (OFET)
organic light emitting diodes (OLED)
organic photo-voltaic cells (OPVC)
electronic paper
different devices made of polymer electronics5,6
Devices

## Slide 14: OFET
Design
OFET are designed like thin film FET2. But:
organic semiconductor
can have organic substrate, insulator, drain and source.

## Slide 15: OFET
0,1
p
Poly(3-alkylthiophen)
0,08
n
C60
1-5,5
p
Pentacene
Charge mobility μ [cm2/Vs]
Structure
Type
Semiconductor
Compounds
Typical organic materials used for OFETs. The best conducting is Pentacen3 (c.f. table left). The mobility is almost comparable with that of amorphous Si (μ =1 cm²/Vs).
It is used in connection with a self-assembled monolayer as gate dielectric, doped silicon as gate and gold source and drain4 (c.f. picture below).

## Slide 16: OFET
Characteristic of an OFET with single grain pentacene as semiconductor and gold electrodes7at temperature T=300K. The channel length is 1µm. We have an on/off ratio of 107.
Characteristics

## Slide 17: OLED
Holes are supplied by anode, going through HTL.
Electrons come from cathode
Electrons and holes meet in the flourescent layer form an exciton.
Recombination of exciton results in light emission2,8
Design and principle
Anode (ITO)
Hole transport layer (HTL)
Fluorescent layer
Cathode (Calcium)
Passivation (epoxy resin)
Electron injection
Electron transport
Exciton generation
Hole transport
Hole injection
Light emission
Exciton recombination

## Slide 18: OLED
(1) R1, R2, R3, R4=alkyl, R5, R6=CN;
(2) R1, R2=alkoxy, R3, R4=alkyl, R5, R6=CN;
(3) R1, R2=alkoxy, R3, R4=alkoxy, R5, R6=H;
(4) R1, R2=alkoxy, R3, R4=alkoxy, R5, R6=H annealed;
(5) R1, R2=alkoxy, R3, R4=alkoxy; R5, R6=CN
wavelength modulation
Fluorescent layer either
  Small molecules
  Polymers
Polymer PPV is easy to manipulate by changing the side chains6.

## Slide 19: OLED
+ printability on almost every surface
+ Flexible substrates
+ OLEDs emit light
=> higher contrast, energy efficient
+ viewing angle >170°
- Lifetime
today

## Slide 20: References
1 Wikipedia, (28.01.2008) http://de.wikipedia.org/wiki/Organische_Elektronik
2 Technische Universität Darmstadt, Poster http://www.tu-darmstadt.de/fb/ms/fg/em/Org.%20Elektronik%20in%20e-mat.pdf
3 Uni Wuppertal, (28.01.2008)
http://www2.uni-wuppertal.de/FB9/poly/ofet.html
4 M.Halik, H.Klauk, U.Zschieschang: “Low-voltage organic transistors with an amorphous molecular gate dielectric”, Nature (2004)
5 K. Bock, Frauenhofer Institutes, “Polymerelectronics”
6 ScherfGroup, “Halbleitende Polymere und …”
7 T.Minari e.a., “Temperature and electric-field dependence of the mobility of a single-grain pentacene field-effect transistor, J. Appl. Phys. (2006)
8 Wikipedia, (28.01.2008) http://de.wikipedia.org/wiki/Organische_Leuchtdiode