Prüfungsfragen 1. Examination

„Semiconductor Technology“

March 3rd, 2008

| 1. | Give at least 3 examples of important semiconductor materials including their major applications and the properties that make them particular interesting for these applications. |  |  | 6P |
| --- | --- | --- | --- | --- |
| 2. | “Thin” films are thin with respect to some length scale defined by system parameters. Give examples for such length scales and discuss briefly possible implications. |  |  | 4P |
| 3. | How would you define the roughness of the two thin films shown in Fig. 1? Give an equation if possible and differentiate between the two cases. |  |  | 6P |
|  |  |  | Fig. 1 |  |
| 4. | The red thin layer (thickness dB) on the blue circular Si wafer substrate (thickness dA >>dB) is under compressive stress ; the wafer thus is warped with a radius of curvature = R as shown in Fig. 2. What would R be proportional to? Explain briefly your reasoning. Hint: This is a two-dimensional problem. |  |  | 6P |
|  |  | Fig. 2 |  |  |

| 5. | Fig. 3 below relates to the nucleation of a thin layer B on a substrate A. a) What is expressed in the ’s and the arrows in this picture and how does it relate to the angle  shown? b) Give the names and simple drawing to the two major growth modes for thin films resulting from considering extremes of ? | 10P |
| --- | --- | --- |
|  | Fig. 3 |  |
| 6. | Go through the essential of Si single crystal growth by the Czochralski (CZ) technique. Give numbers as far as possible and discuss topics like in-situ doping, keeping the crystal dislocation-free, and problems due to segregation. | 10P |

| 7. | Give a plot of the doping atom concentration as a function of depth z for the kind of transistor shown in Fig. 4. Describe the plot qualitatively but give some numbers on the axes’ as far as possible. Consider carefully how you plot doping concentration - Indicate the pn junctions in your drawing. Discuss their depth and distance in terms of process stability. - Describe how the doping could be administered. - Discuss possible problems encountered, in particular if the substrate doping is rather high. |  | 13P |
| --- | --- | --- | --- |
|  | Fig. 4 |  |  |
| 8. | Draw a schematic cross-section of two complementary CMOS transistors next to each other. Indicate the major difference to MOS. |  | 12P |
| 9. | Give 2-3 examples of MEMS products, their working principles and range of applications. |  | 6P |

| 10. | In an evaluation of capacitive forces for driving MEMS devices we consider the two situations shown in Fig. 5. The zero point of the x-axis denotes the position of the light blue plate at rest, i.e. without a voltage applied as shown. We consider only movements in the x-direction as shown for the two configurations given (where the plates have moved some distance x from their equilibrium position. a) Show that the force F pulling at the moveable plates for both configurations for an applied voltage U is given by F = -(U2/2)  (dC/dx) - kx Hint: Consider the work W = U I dt needed to move a plate and remember that force F = –dW/dx and C = Q/U = A/distance, I = dQ/dt. b) Derive the proper expressions for C with the parameter given and compare the relative strength of the two configurations (you may assume that y  yd) c) Discuss the pros and cons of the two configurations for driving an actual actuator. |  | 16P |
| --- | --- | --- | --- |
|  |  | Fig. 5 |  |
| 11. | Give some rough numbers (with some reasoning wherever applicable), always per m2, for - Maximum solar power. - Maximum and practical efficiency of "standard" Si solar cells. - Average power for "standard" Si solar cell. - Average energy harvest of "standard" Si solar cells per year. |  | 9P |

| 12. | a) Draw the current (density) –voltage characteristics of an “ideal” solar cell (with approximate numbers as far as possible. b) Identify in the drawing the three major parameters that describe the solar cell (efficiency). c) Draw in the same diagram (qualitatively) the IU power curve and identify the optimal working point | 11P |
| --- | --- | --- |
| 13. | a) Draw the equivalent circuit diagram of a “real” solar cell b) Discuss the influence of series or shunt resistors by drawing - a current (density) –voltage characteristics with only series resistors (i.e. RSH = ). - a current (density) –voltage characteristics with only shunt resistors (i.e. RSE = 0). c) Give brief reasons for your choice of curves in both cases. | 14P |
| 14. | a) What is the idea behind "concentrator cells"? b) Discuss the basic principle and necessities (including money-related topics) concerning applications. | 7P |
| 15. | The picture shows a schematic "to scale" drawing of a simple blue Laser diode and the relevant material parameters in the "master" diagram - What kind of approximate band gap energy can you assign to the various layers? Draw a schematic band diagram of this kind of situation. - Which layer is the light-producing one? - What is the function of the three relatively thin layers in the center region? - What could be the function of the two thicker pure GaN layers? - Why is the whole structure on an Al2O3 substrate (= sapphire) and what is the electrical problem encountered? - What might be the problem necessitating a "buffer" layer between the Al2O3 substrate and the stack of functional layers? - Where are the mirrors necessary for a Laser? - What is obviously used for n- or p-doping? Make a guess as to why the very thin central layer contains Mg and Si as dopants | 20P |

|  | Fig. 6a) |  |  |
| --- | --- | --- | --- |
|  | Fig. 6b) |  |  |